## Slide 1
FAM 8.12.2017
Leon Camenzind

## Slide 2: Motivation
Technical: Calibration routines --> scaling up (paradigm for «virtual gates») Baart et al., APL108 (2016) «Computer-automated tuning of semiconductor double quantum dots into the single electron regime»
Isolated vs. collective Coulomb blockade Stafford and Das Sarma, PRL72 (1994): «Collective Coulomb Blockade in an Array of Quantum Dots: A Mott-Hubbard Approach”
Cold atoms: Landig et al., Nature 532 (2016)
Establish quantum dot arrays as quantum simulatons plattform

## Slide 3: Fermi-Hubbard Model
: nearest neighbor
t
t
: Fermionic creation/annihilation op.
+U
Tight-binding
On-site coulomb
Spin density operator for site i:
Dot occupation operator:

## Slide 4: Mott-Hubbard Insulator
Transition metal oxides are insulators
Tight-Binding/LCAO  metal
+ Hubbard U  insulator
Mott gap:
NiO: competiion U and t in 3d orbitals

## Slide 5: Extented Fermi-Hubbard Model
Spin density operator for site i:
Dot occupation operator:
: nearest neighbor
t
t
+U
Tight-binding
On-site coulomb
: Fermionic creation/annihilation op.
Inter-site coulomb

## Slide 6: Setup and Hubbard model
Full (independent) control over parameterspace: define virtual gates linear combinations of physical gates 1. 2. Measure 3. Simulation of Hubbard-Model using extracted & calibrated parameters
Intra-dot Coulomb
Inter-dot Coulomb
Hopping
Dot energy
Toolbox

## Slide 7: Uniform filling of the array
Y-Axis: Combination of all seven gates (only values shown)
Tunnel couplings constant
Isolated Coulomb blockade
Reservoir
Dot-Dot
Equal sweep of local fillings
Detuning of outer dots

## Slide 8: 1. Virtual gates: separate variables in parameter space
(measured from polarization lines)
: crosstalk (measured from charge transitions)
Virtual plunger gates
Virtual barrier gates

Matrix measured for variety of electron fillings
Matrix measured for different interdot-couplings
Controlling Hubbard model means independent control of

## Slide 9: 1. Leverarm and tunnel coupling
(a) PAT strong coupling: DD hybridized charge state spectrum (bonding – antibonding)
(b) Polarization line width The excess charge transition is broadened both by an effective electron temperature and by the tunnel coupling
with
[1] Oosterkamp et al., Nature 395 (1998)
[1]

## Slide 10: 2. Calibrated charge-stability diagram and and barriers
= adding of second electron into shell
: with vs.
Change only or (other TB + unaffected)
)
Virtual plunger gate
Virtual barrier gate

## Slide 11: Simulations of collective Coulomb blockade for the simplified Hubbard model
Here: no inter-dot Coulomb ()
: addition peaks triple degenerated (same addition cost)
: peaks split into “miniband” breakdown of Coulomb blockade in dots. But energy still gapped. Delocalized electrons: no good quantum number anymore.
Merging of bands
Limit: Merging into one large dot
Electron addition spectrum

## Slide 12: Collective Coulomb blockade
Homogenious filling by tune vs.
: inter-capacitance lifts degeneracy of addition peak at
: ( becomes bad quantum number. GS superposition of different charge states
Minibands collapse  from Mott insulator to metallic state
Comparison to theory: Measure and calc. from extended Hubbard model.
Collective Coulomb blockade physics in the Fermi–Hubbard phase space

## Slide 13: Transport signatures
large dot: collective Coulomb blockade
in miniband
in in Mott gap

## Slide 14: Summary
From isolated to collective Coulomb blockade by increasing hopping term
Proof of concept for completely separeted tuning of involved energies
Proof of a quantum simulator for a many-body problem in a semiconductor quantum dot array

## Slide 15: Thank you for your attention

## Slide 16: 3d Orbitals

## Slide 17: Miniband width and electron temperature

## Slide 18: Determining lever arm and tunnel coupling

## Slide 19: Model parameters
weight in superposition