## Slide 1
12.01.2018
Taras Patlatiuk
Zumbühl Group
Spin wave (magnons) transport in a quantum Hall ferromagnet
D. S. Wei, T. Van der Sar, S. H. Lee, K. Watanabe, T. Taniguchi, B.I. Halperin, & A. Yacoby

## Slide 2: Motivation
  Spin waves transmit information without displacing charge
  Study highly correlated states (frac. QH, bilayer graphene)
  Spin superfluidity in Canted Antiferromagnet (CAF)
  Bose-Einstein condensate of magnons
  Magnons are charge-neutral: challenging to detect and study

## Slide 3: Device
hBN/graphene/hBN
Scale bar: 1 µm
Dashed white lines: graphene flake
Solid yellow: leads (Ti/Au)
Transparent yellow: top gates
  graphene (small SOI) -> long-lived spin waves

## Slide 4: Spin wave generation
Bulk in tuned to ν = 1 (ferromagnetic)
Contact doping: additional edge states
Spin wave excitation energy: EZ=gµBB
µ = -eVdc
Reverse process affect conductance
(redistribute chemical pot.)
Do not equilibrate
Equilibrate

## Slide 5: Verification using top gate

## Slide 6: Tilted magnetic field
Relevant field: total B
EZ = gµBB
Previous study: only depends on B⟘ (exchange gap excitations)

## Slide 7: Two terminal conductance
i - amount of redistributed chemical potential
i -proportional to the amount of absorbed magnons
Closer to the generation – stronger i

## Slide 8: Relative magnon absorption
dI/dV = dIP/dµ
IP = - I/e

## Slide 9: Non-local voltage signal

## Slide 10: Conclusion
  Magnon generation, propagation, detection
  Unimpeded propagation through ν=0/ν=1 interface
  Magnon propagation through insulating canted antiferromagnet

## Slide 12: Magnons in quantum Hall ferromagnet

## Slide 13: Non-local CAF