## Slide 1: Spin-orbit interaction in a dual gated InAs/GaSb quantum well
A. Beukman et al. (Kouwenhoven Group) arXiv:1704.03482
Kris Cerveny
19.05.2017
Friday Group Meeting Talk
Notes: Logo of PASPS9 conference

## Slide 2: Introduction
Investigates SOI in dual-gated InAs/GaSb quantum well
Tune between single and double carrier regimes ( and + holes)
Analyze difference in density of SO split bands
Extract zero-field density difference
SOI near hybridization gap
Motivation:
InAs and GaSb have strong SOI
Rashba strength tunable with gating for InAs
Control of SOI necessary for spintronic devices
Strong SOI + large g-factor + inducible superconductivity ingredients for topological superconducting phase
Experiment:

## Slide 3: InAs/GaSb DQW
InAs + GaSb  Interesting band structure [1]
GaSb valence band maximum higher in energy than InAs conduction band minimum [2]
Energy range where in InAs coexist with holes from the GaSb
Strong coupling  -hole hybridization  gap when
[1] F. Qu et al., PRL 115, (2015)
[2] H. Kroemer, Physica E 20 (2004)

## Slide 4: Sample
20μm x 80μm Hall bar
300mK Measurements
GaSb substrate lattice matched with subsequent layers  no need for thick buffer as with GaAs  better coupling between BG and wells!
[1] F. Qu et al., PRL 115, (2015)

## Slide 5: as function of
2T out of plane magnet
High (dashed lines)  inside gap
Green line separates single- and dual-carrier regimes
Line : mobility highest Line : close to hybridization gap

## Slide 6: Electron-only Regime
Trace along line (fixed density)
Clear SdH oscillations in  beating pattern as function of
SdH osc. for each spin band periodic in
System favors one SO eigenstate  
Trends from 1-10:
  Extra frequency peak
    Asymmetry between beats (amplitude and oscillation #)
  Decreased spacing of peaks (decreasing )
    Increasing # of oscillations in A & B  nodes pushed to lower B fields

## Slide 7: Center Frequency Peak
Emergent central peak does not correspond to a density
3 possible mechanisms can cause extra freq. components:
  Magnetic inter-subband scattering
  Magnetophonon resonances
  Magnetic breakdown
Emergent central peak does not correspond to a density
3 possible mechanisms can cause extra freq. components:
  Magnetic inter-subband scattering
  Magnetophonon resonances
  Magnetic breakdown:
     Carriers tunneling between spin polarized Fermi-surfaces
[Schematics] W. G. Chambers, Proc. Phys. Soc., Vol 84, 1964

## Slide 8: Simulation vs Measurement
[4] R. Winkler, Spin-orbit Coupling Effects in Two-dimensional
Electron and Hole Systems, Springer 2003
Compare data to QM LL simulations with the MB mechanism [4]
Solve for LL energies and extract
Parameter tuning yields:
Cubic Dresselhaus term set to zero for good fits!?!?
In 2D systems:
 Valid for infinite square well…

## Slide 9: Two Carrier Regime
in InAs present with holes in GaSb simultaneously
Investigate influence of hybridization on through magnetoresistance traces on line
Hole concentration increases from point 1 to 13  13:
      near hybrid. gap

## Slide 10: Magnetoresistance Data
Traces with and without beating
 no beating  no ZFDD extractable
Non-monotonic behavior!
Band structure calculations agree qualitatively for first 10 points

## Slide 11: Lack of Beating
Two possible reasons:
  Strong asymmetry between spin species determines visibility ()
[5]
[5] J. Luo et al., PRB, 41, (1990)
[6] F. Nichele et al., ArXiv (2016), 1605.01241
    When approaching hybrid. gap and are very dissimilar  visibility reduced below experimental detection limits
  Energy window with single spin band present [6]
    No beating possible
They can not determine which is the cause

## Slide 12: Conclusion
Study of SOI in InAs/GaSb DQW by top and back gating
Tunable in electron-only regime  extract Rashba and Dresselhaus
Non-monotonic spin splitting behavior in two carriers regime  crossing of spin bands due to hybridization

## Slide 13
Thanks for listening!!

## Slide 18
Christopher Schierholz – Rashba Spin-Orbit Interaction in Low and High Magnetic Fields