## Slide 1: James Mingchi Xu 30.08.2024
Journal Club - Zumbühl Group

## Slide 2
Outline
The device Architecture
Characterization of QPCs
Coulomb Diamond in Different Tuning Regime
Measurement with the Charger Sensor
The connection to the Microkelvin project.

## Slide 3: Device architecture
Electron Density: 2× cm2
Mobility: 2×106 cm2/V*s
Area: 2.6 µm2
Level spacing: Δ = 2.7 µeV (31.11mK)
To calculate the self capacitance and the charging energy (naively):
C0=8ϵ0 ϵr R = 8.351e-16F
where ϵr = 13.1, and R = 0.9 µm (A disc charge with same area in infinite GaAs)
Ec = e2/C0 = 2.22K * kb

## Slide 4: Characterization of QPCs
The exact voltage of Vn is not specified :(
The sub-band spacing of is around 50µeV (0.58K)

## Slide 5: Characterization of QPCs
T = 540 mK
B = 25 mT
Tunnelling regime
Tunnelling regime
1st plateau
1st plateau
1st plateau
T = 13 mK ; B = 25 mT ; 1mV period

## Slide 6: Coulomb Diamond in Different Regime
T = 13 mK ; B = 0 mT
For Vn < -370mV
Ec = 115µeV (1.33K)
For Vn = -315mV
Ec = 16µeV (180mK)

## Slide 7: Coulomb Diamond in Different Regime
T = 13 mK ; B = 0 mT
When both QPC’s are kept on the first plateau…

## Slide 8: Charging Energy Renormalization (Ref[6,7])

## Slide 9: Measurement with the Charger Sensor
Model from ref[10]
Mesoscopic charge quantization
I. L. Aleiner and L. I. Glazman
Phys. Rev. B 57, 9608 – Published 15 April 1998

## Slide 10: Measurement with the Charger Sensor

## Slide 11: Conclusion
Coulomb blockade caused by weak localization is observed.
The charging energy of a QPC defined quantum dot changes significantly with the tuning.

## Slide 12: The A 2DEG CBT
Ohmic
Ohmic
QPC
QPC
To park the QPCs on the plateau?
The dimension of the charging island?
The charging energy renormalization?
To use the WL as the charging effect?
Shape of the island?
Quantum hall regime?