## Slide 2: Why Singlet-Triplet? Why holes? Why MOS?
Singlet-Triplet
+ Low B (<5 mT)
+ No GHz (baseband)
- Footprint
- Complex eigenstates
Holes
+ Large intrinsic SO
+ Tunable g-factor & SO
+ Suppressed hyperfine
+ Potential sweet spot
- Large intrinsic SO
Silicon MOS
+ Scalable
+ CMOS compatible
- Bad interface
- Charge Noise
Anisotropic exchange coupling!
Theory predicts leakage error prevention?
ST hole qubit in Silicon MOS not yet shown!

## Slide 3: Device & Fabrication
ΓL > 10 MHz, ΓR < 30 kHz, tc > 1 GHz

## Slide 4: Charge Stability Diagram

## Slide 5: Singlet-Triplet & Readout

## Slide 6: Magnetospectroscopy
tc = 9 ± 1 μeV
Eff. g-factors:
0.8 ± 0.1
1.2 ± 0.1

## Slide 7: Anisotropic g-tensors

## Slide 8: Anisotropic g-tensors

## Slide 9: Anisotropic of the FFT amplitudes

## Slide 10: Coherent Δg-driven oscillations
J = 6 MHz @ ϵ = 1.9 meV
∣Δg∣ = 0.41

## Slide 11: Coherent Δg-driven oscillations

## Slide 12: Dephasing
δϵ = 30 μeV and δΔEZ = 4 neV

## Slide 13: Coherent exchange-driven oscillations

## Slide 14: Coherent exchange-driven oscillations

## Slide 15: Spin-echo measurement
T2Echo = 550 ± 50 ns @ 0 echo
T2Echo = 1220 ± 150 ns @ 1 echo
T2Echo = 1300 ± 200 ns @ 2 echos

## Slide 16: Conclusion
Characterized Anisotropic g-tensors and tSO
Shown coherent Δg-driven oscillations
Shown coherent exchange-driven oscillations
Demonstrated spin echo pulse