## Slide 1
Journal Club
Presenter: Maryam Taghilou
Date: 18.06.2026

## Slide 2
Tunnel junction applications
Josephson junctions
SIS
• Superconducting qubits
• SQUIDs
Thermometers
Normal and hybrid junctions: NIN / NIS
• CBTs
• Shot-noise thermometers
• NIS thermometer
Detectors
Hybrid junctions: NIS / SIS
• bolometers
Electronic coolers
NIS junctions
• Selective extraction of hot electrons

## Slide 3: Junction paramter manipulation
Fabrication-stage control
Design parameters such as junction area
Oxidation time
Temperature: Annealing or cooling down during fabrication
Post-fabrication manipulation
Annealing: heating, Laser, Ebeam
Alternating bias assisted annealing (ABAA)

## Slide 4
Nb 200 nm/Al 7 nm–AlOx15 mins /Nb 100nm.
Annealing for 1 hour.
Area: 2-3 um2
Examples of Manipulation using Anealing:
Nb/Al–AlOx /Nb
130nm/10nm/30nm
Oxidation time: 1h
Junction Area: 4 um2
200C
220C
240C

## Slide 5
Al 55nm–AlOx(thermally grown in situ in pure oxygen at 0.2–0.5 mbar for 3–5 min)–Al samples were annealed between 350 and 450 °C.
junction area of 0.05 or 0.15 um2 . 1 to 100 kohm. increased 1.5–3 times . supercurrent is reduced in accordance with the increase of tunneling resistance.

## Slide 6: Jun:150×600 nm2,0.1 mbar,oxidation,Al.AlOx.Al 15/45nm
focused Ar+ laser beam , A thermographic imaging allows controlling the temperature distribution
30 s at T=170 °C reduction of 40% of the critical current Ic going from 120 to 70 A. 13.6 to 21.6 ohm.
The Josephson junctions are window-type with an area of 4*4 um2 and separated by 14 m. A beam spot of 30u m
2.22*10ˆ5 W/cm2 ,landa= 500 nm
Increasing resistance up to 60% from 13.6 to 21.6
reduceing the resistance spread 3.11 % to 1.48 %
Dose: 50 uC/cm2, Right field: 0.25 um2

## Slide 7
Cabrera–Mott model
• Adsorbed ionic oxygen makes an intrinsic electric field of ~1 GV/m. • This field drives Al³⁺ and O²⁻ in opposite directions, producing conformal, self-limiting oxide growth. • The characteristic potential is the Mott voltage, ≈ 0.5–1 V for AlOₓ.
ABAA Method:
Applying alternating voltages in the order of after fabrication

## Slide 8: Resistance Manipulation
Voltage Pulses +-
Annealing at 80C gives maximum R change
Vm=0.9 V, 1s
VA=10 mV 0.5 s
R= 10 kohm
Areaj= 1.5*0.2 um^2

## Slide 9
Manupulation of
Transmon Qubit Frequency
Manipulation of Transmon Qubit Frequency
Tunability of Qubit frequency
ABAA
no ABAA
No TLS coupling with Transmon
Absence of TLS coupling in ABAA treated samples
Ic: 20 to 30 nA

## Slide 10
Initial Resistance drop
Resistance grows with pulsing
Logarithmic R growth after pulsing is stopped
Manipulation Protocol
150 nm*600 nm

## Slide 11: Voltage-Pulse Manipulation and Resistance Drift
Applying train of pulses
No pulse during t_Relax
Resistance increase up to 270%
270% corresponds to 2 GHz
Blank t: 100ms, palse t: 200 ms, measure t: 20 ms

## Slide 12: Effect of Oxidation Dose on Resistance increase
Three different junctions
Lower oxidation dose max manipulation

## Slide 13
How to decrease the resistance after ABAA?
After ABAA:
Annealing in N2: Resistance decreases both at and
Annealing in ambient: Resistance increases at but decreases at

## Slide 14: Summary
Effect of ABAA on junctions with different oxidation dose Max change (270%)  minimum oxidation dose
Annealing in N2 reverses the resistance change after ABAA
Thank you for your attention

## Slide 15: Appendix

## Slide 18
two coupled “reservoirs”: an internal reservoir and an external reservoir
Aging Effect in Different environments: